## Slide 1: Radiation Effects on CMS PbWO4Crystals and Consequences for Physics
Kristina Hanna
University of Southampton
Master’s project presentation
5 June 2017

## Slide 2: CMS Detector

## Slide 3: Compact Muon Solenoid (CMS)
General-purpose detector at the LHC
Designed for Higgs boson discovery and search for new physics
Comprised of subdetectors with different functions

## Slide 4: Electromagnetic Calorimeter (ECAL)
Hermetic subdetector designed to make high resolution measurements of e- and γ energy
Consists of:
  Barrel (36 Supermodules)
  2 Endcaps (2 “Dees” each)
  Preshower (2 plates of lead each with a layer of silicon sensors)
Contains 75 848 PbWO4 crystals:
  14 648 in the endcaps
  61 200 in the barrel
My study focuses on the ECAL endcaps
Structure of the Electromagnetic Calorimeter

## Slide 5: PbWO4 Crystals
Radiation-tolerant
Excellent energy resolution
Fast signals
Compact shower containment
Dimensions: 3 x 3 x 22 cm3
Grown by 2 different crystal producers:
  Bogoroditsk Techno-Chemical Plant (BTCP), Russia
  Shanghai Institute of Ceramics (SIC), China
Picture of a PbWO4 crystal with an early Vacuum Phototriode

## Slide 6: Vacuum Phototriodes (VPTs)
Used in EE for scintillation light detection
Gain ~ 10
1 inch diameter
Radiation-hard
Designed to work in axial magnetic fields
Cannot operate in strong transverse magnetic fields
Picture of a mass-production Vacuum Phototriode

## Slide 7: ECAL Role in Higgs Discovery
H → γγ H → ZZ* → 4l

## Slide 8: My Project

## Slide 9: Overview
Even though radiation-hard, ECAL crystals suffer from damage in the harsh LHC environment.
Important to understand loss of response, its impact on physics, and make predictions for the future.
Endcaps experience higher radiation, and therefore more damage.
Studying EE can preview what’s going to happen in EB in the long run.

## Slide 10: Contributions to Response Loss
Ionisation (dE/dx) damage:
  Occurs due to creation of colour centres.
  Spontaneous annealing at room temperature.
Hadron damage:
  Hadrons hitting nuclei and causing crystal lattice damage, reducing the crystal transparency.
  Anneals only at high (~300 °C) temperature.
  Considered permanent in ECAL.
VPT conditioning
  Predicted to lose ~30% response due to the absorption of the residual gas in the imperfect vacuum on the photocathode.
  Linear recovery of ~10% per year.
VPT faceplate darkening
  Occurs due to creation of colour centres.
  Irreversible; expected to contribute up to 10% to the response loss.

## Slide 11: Laser Data
Data collected by ECAL laser calibration system:
  Use blue laser light of λ = 447 nm.
  Measured every 45 min over the 75 848 crystals.
  Normalised to the response in March 2011.
Purpose – to normalise ECAL physics response.

## Slide 12: Channel Response Loss
Response to laser light (447 nm) with respect to unity in March 2011.
|η| < 1.4 – barrel region; |η| > 2.7 – crystals closest to the beam pipe.
Damage during LHC fills;
Recovery during LHC off-periods
Channels in higher radiation levels have lower response.

## Slide 13: Channel Response Loss
Response loss decomposition into 4 different components.
Predictions for |η| > 2.7.
Vertical line corresponds to the integrated luminosity in CMS at the end of 2016.
Currently 3 effect play an important role:
  dE/dx damage;
  Hadron damage;
  VPT conditioning.
Image credit: Butler, A. (2014). Evolution of the CMS Electromagnetic Calorimeter Endcap Response at the LHC (Master’s Thesis)

## Slide 14: Project Outline
Analysing laser data to follow channel response over time and its dependence on η.
Modelling channel response recovery, calculating:
  Recovery Time Constants
  Projected recovery
Comparison between:
  BTCP and SIC crystals
  Same producer crystals in different η regions
Comparison of the findings with crystal and VPT properties

## Slide 15: Motivation
~60% of H → ZZ* → 4l events involve the endcaps.
Losing response in parts of EE – losing some events.
Predictions for EE crystals before Phase II Upgrade.
Insight into EB crystal behaviour in the future.
Acceptance of H → ZZ* → 4l events as a function of η coverage

## Slide 16: Laser Data Analysis

## Slide 17: Crystals Used in the Study
Each endcap 100 crystals in diameter.
1 crystal corresponds to 1 unit in x and y.
Two crystal producers:
  BTCP (green)
  SIC (red)
Five crystal sets used for:
  Comparison between BTCP and SIC
  Comparison between η regions
  Comparison between EE- and EE+
Notes: Give EE dimensions in real life
(At the start) show a photo of the endcaps so that people can relate to the real life image.

## Slide 18: Comparison of BTCP and SIC crystals
Notes: Draw arrows to the graph from the right, stating what’s where: difference plot; reference line; luminosity.

## Slide 19: Comparison of BTCP and SIC crystals
Similarities:
  Relationship between the channel response and the luminosity
  Correlation between BTCP and SIC crystals
Differences:
  Differences in the rates of damage and annealing during and outside the LHC fills
  Long term crystal behaviour
  Response of the SIC channels is consistently lower than that of the BTCP channels.

## Slide 20: Comparison of Different η Regions
Notes: Again, explain the plot. Same as slide 16.

## Slide 21: Comparison of Different η Regions
Similarities:
  Relationship between the channel response and the luminosity
  Recovery level decreases as the channel response decreases
Differences:
  Response loss depends on η
  Channels at higher η recover less

## Slide 22: Laser Response Overview
Qualitatively same trends for all crystals.
BTCP response higher than SIC.
BTCP crystals have higher recovery levels than SIC in the same η region.
Channel response and recovery levels depend on η and hence the radiation levels.
Channels in EE+ were found to have the same trends with their channel response lower by ~0.025.

## Slide 23: Crystal Recovery Modelling

## Slide 24: Crystal Annealing
Recovery process:
  Most recovery due to dE/dx;
  Colour centres anneal at room temperature;
  Thermal process can be described by an exponential function;
  VPT recovery negligible.
Single exponential formula used:
τ - Recovery Time Constant (RTC).
The data were fit using ROOT least χ2 algorithm.
Notes: Include plot: top graph from Fig. 24 (report)
Give formula: put τ in red so it stands out; can’t do in formula so work out how to.

## Slide 25: Recovery Modelling
Eight recovery periods fitted.
Recovery periods had to have substantial amount of data without unexplained jumps.
Single exponential was sufficient for the 8 periods chosen.

## Slide 26: Recovery Time Constants
RTC results
Characteristic recovery of one colour centre ~50 h.
RTC appears coherent for the 5 sets.
Periods with different results:
  5 includes a short LHC fill;
  8 includes heavy-ion run.
Notes: Add arrows to the graph at 100 h and 500 h, state: 4 and 20 days.

## Slide 27: Projected Recovery
Projected recovery depends on the response level of the channel.
The crystals only recover by up to 10% of they March 2011 response.
EE will be replaced in ~2024 due to the radiation damage.
EB crystals are expected to see similar effects in the long run.

## Slide 28: Consequences to Physics

## Slide 29: Consequences to Physics

## Slide 30: Consequences to Physics
Notes: Same figure, same size but this time with circles for an example

## Slide 31: Ageing Contribution to Resolution
Current levels in the inner EE rings dropping below 0.1.
By the end of the current EE life, from the predictions the resolution will degrade from ~2% to ~3.2%
With similar effects expected in EB, resolution would degrade from current ~1% to ~2.7%.
Need to keep checking the laser data to make sure we’re still with the predictions.

## Slide 32: Conclusions (and Future Work)

## Slide 33: Conclusions (and Future Work)
Crystals do not recover completely.
Differences between BTCP and SIC.
Differences between different η regions.
Could be showing that hadron damage is starting to play a significant role.
Can learn more with more data – previous and future, and using more crystal sets.

## Slide 34: Thank you

## Slide 35: Backup

## Slide 36: VPTs and APDs
Vacuum Phototriode
Avalanche Photodiode
Used in EB
Gain ~ 50
5 x 5 mm (2 per crystal)
Leakage currents in high radiation environment
High resolution
Used in EE
Gain ~ 10
1 inch diameter
Radiation-hard
Cannot operate in strong transverse magnetic fields

## Slide 37: Motivation
Main Higgs discovery channels
Give the two highest cross-section Higgs creation Feynman diagrams

## Slide 38: Laser Response Overview

## Slide 39: Projected Recovery
Asymptotic recovery results

## Slide 40: Crystal and VPT Properties
Properties used:
  Lighy Yield (LY), [p.e./MeV]. A measure of the amount of scintillation light crystal produced before irradiation. Measured for all EE crystals.
  Index of Induced Absorption (μ), [m-1]. Inverse of radiation hardness of the crystal. μSIC measured by SIC for all SIC crystals except 2 SCs; μECAL measured by ECAL for a fraction of BTCP and SIC crystals.
  VPT quality. Product of VPT gain and quantum efficiency of the VPT. Measured for all VPTs.

## Slide 41: Induced Absorption and Laser Response
Hind of correlation observed
Shouldn’t be expected because:
  Hadron damage appears to be starting to dominate
  Inaccuracies in measurements
  Many contributing factors